AASHTO SOIL CLASSIFICATION SYSTEM

Developer Logic & Classification Rules  |  AASHTO M 145 / ASTM D3282

Cransfield Materials Testing Centre  |  Reference: Table 5.1

# 1.  Purpose

This document defines the exact logic required to implement the AASHTO M 145 soil classification algorithm in any programming language. It covers: required inputs, step-by-step decision rules, Group Index (GI) calculation, and test cases for validation.

# 2.  Required Inputs

The classifier requires the following sieve analysis and Atterberg limit values:

| Variable | Sieve / Test | Description | Limit used in classification | Required? |
| --- | --- | --- | --- | --- |
| P10 | No. 10 (2.00 mm) | % of soil passing No. 10 sieve | A-1-a: P10 ≤ 50 max | Required for A-1-a check |
| P40 | No. 40 (0.425 mm) | % of soil passing No. 40 sieve | A-1-a: P40 ≤ 30 max A-3: P40 ≥ 51 min | Required for A-1-a and A-3 checks |
| P200 | No. 200 (0.075 mm) | % of soil passing No. 200 sieve — the PRIMARY SPLIT | ≤ 35% = Granular > 35% = Silt-clay | Always required |
| LL | Atterberg (No. 40 fraction) | Liquid Limit measured on fraction passing No. 40 | Used in A-2, A-4 to A-7 routing | Required when P200 > 25% |
| PI | Atterberg (No. 40 fraction) | Plasticity Index on No. 40 fraction. Enter 0 for NP. | Used in all group splits | Required when P200 > 25% |

CRITICAL NOTE: ALL THREE sieve values (P10, P40, P200) are required for correct classification of granular soils. The No. 40 sieve (P40) is used both as a minimum criterion for A-3 (≥ 51%) and a maximum for A-1-a (≤ 30%) and A-1-b (≤ 50%). LL and PI are still measured on the fraction passing No. 40. If P40 data is unavailable, A-3 cannot be confirmed and A-1-a cannot be fully verified.

# 3.  Classification Groups — Quick Reference

The AASHTO system produces 12 possible group classifications. All criteria must be satisfied for a group assignment:

| Group | P10 (%) No.10 | P40 (%) No.40 | P200 (%) No.200 | LL (%) | PI (%) | Material type | GI | Rating |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| A-1-a | ≤ 50 | ≤ 30 | ≤ 15 | — | ≤ 6 | Stone fragments, gravel, sand | 0 | Excellent–Good |
| A-1-b | — | ≤ 50 | ≤ 25 | — | ≤ 6 | Stone fragments, gravel, sand | 0 | Excellent–Good |
| A-3 | — | ≥ 51 | ≤ 10 | — | NP | Fine sand | 0 | Excellent–Good |
| A-2-4 | — | — | ≤ 35 | ≤ 40 | ≤ 10 | Silty or Clayey Gravel sand | 0 | Excellent–Good |
| A-2-5 | — | — | ≤ 35 | > 40 | ≤ 10 | Silty or Clayey Gravel sand | 0 | Excellent–Good |
| A-2-6 | — | — | ≤ 35 | ≤ 40 | > 10 | Silty or Clayey Gravel sand | 0–4 | Excellent–Good |
| A-2-7 | — | — | ≤ 35 | > 40 | > 10 | Silty or Clayey Gravel sand | 0–4 | Excellent–Good |
| A-4 | — | — | > 35 | ≤ 40 | ≤ 10 | Silty soil | 1–8 | Fair–Poor |
| A-5 | — | — | > 35 | > 40 | ≤ 10 | Silty soil | 1–12 | Fair–Poor |
| A-6 | — | — | > 35 | ≤ 40 | > 10 | Clayey soil | 1–16 | Fair–Poor |
| A-7-5 | — | — | > 35 | > 40 | ≤ LL−30 | Elastic clayey soil | 1–20 | Fair–Poor |
| A-7-6 | — | — | > 35 | > 40 | > LL−30 | Plastic clayey soil | 1–20 | Fair–Poor |